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TABLE 1: REGISTERED DESIGNATIONS AND CHEMICAL COMPOSITION LIMITS FOR POWDERS1,2,3,4,5,6
	
	Alloy Designation and Chemical Composition Limits Registered Since the 2025 Edition

	
	Designation
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	Al

	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	
	

	
	AA No.
	Date

REGISTERED
	PRODUCTS
	Si
	Fe
	Cu
	Mn
	Mg
	Cr
	Ni
	Zn
	Ti
	O
	Be
	Pb
	Sn
	Zr
	Others
	FNs
	Each4
	Total4
	  Minimum

	
	2A09.50
	07/06/2026
	Powder
	0.25
	0.20
	3.2-4.4
	-
	1.0-1.6
	-
	-
	0.10
	-
	0.06
	-
	-
	-
	-
	-
	-
	0.05
	0.15
	Rem.

	
	6A63.50
	02/17/2026
	Powder
	0.25-0.6
	0.35
	0.10
	0.10
	0.40-0.75
	0.10
	-
	0.10
	0.10
	0.45
	-
	-
	-
	-
	Co: 0.10
Na: 0.10
	10
	0.05
	0.15
	Rem.


TABLE 2: CALCULATED THEORETICAL DENSITIES OF ACTIVE POWDERS
	
	Density

	Designation
	lbs/cu.in.
	kg/m3 x 103

	2A09.50
	0.099
	2.75

	6A63.50
	0.097
	2.69


Unless specified below, for all referenced footnotes refer to the Purple Sheet as applicable.
FN4, “Others” includes listed elements for which no specific limit is shown as well as unlisted metallic elements.  The producer may analyze samples for trace elements not specified in 

the registration or specification.  However, such analysis is not required and may not cover all metallic “Others” elements.  Should any analysis by the producer or purchaser establish that 

an “Others” element exceeds the limit of “Each” or that the aggregate of several “Others” elements exceeds the limits of “Total”, the material shall be considered non-conforming.
FN10, Co and Na are intentionally controlled to ensure the minimization of radioactive nuclides.

